## Slide 1
Proximity Effect in EBL
by:
Abhay Kotnala
January 2013
Electrical and Computer Engineering Department
University of Victoria

## Slide 2
Outline
Introduction
Proximity Effect: A Physical Insight
Proximity Effect:Avoidance& Correction
Conclusion
References

## Slide 3: Introduction
“Encyclopaedia Britannica on head of a pin”
Proximity Effect is inherent problem associated with EBL
Studied extensively theoretically and experimentally

## Slide 4
Proximity Effect
The proximity effect is the change in feature size of pattern as a consequence of non uniform exposure in regions adjacent to those addressed by the electron beam
Pattern affected by proximity (left), After elimination of proximity effect (Right)

## Slide 5: Consequences
Limits the resolution of EBL
Imposes restriction on the size and shape of the structures
Other Effects
  Corners in the desired pattern become rounded
  Gap spacing and line width are modified
  Features may merge together or disappear completely

## Slide 6: Electron Interactions: A Physical Insight
Electron enter the resist and penetrate further into the substrate
Types
  Forward Scattering
  Backward Scattering

## Slide 7: Continued
Forward Scattering
  Inelastic scattering
  Small Scattering angle
  Widening of the electron beam
  Small contribution to proximity effect
Backscattering
  Elastic scattering
  Large scattering angle
  Additional exposure to the resist in adjacant areas
  Large contribution to proximity effect

## Slide 8: Proximity Effect(Revisited)
Direct consequence of Electron Scattering
Nonuniform distribution of actually receieved exposure by the incident electron beam
Two types of proximity effect
  Intraproximity Effect
  Interproximity effect

## Slide 9: Avoidance and Correction
Improved/Optimized Mask Design
Optimize Exposure and Development condition
Effective process measure
  High energy electron beam
  Thin resist
  Low atomic number substrate
  Thin substrate
  Multilayer resist processes
Utilize proximity correction software
  Exposure dose modulation
  Shape dimension adjustment technique

## Slide 10
Conclusion
Most challenging problem in e-beam lithography
The physical phenomenon of electron scattering responsible for proximity effect.
There exists a trade-off in proximity effect correction between speed, complexity and accuracy.

## Slide 11: References
Chang, T. H. P. (1975). "Proximity effect in electron-beam lithography." Journal of Vacuum Science and Technology 12(6): 1271-1275.
Browne, M. T., P. Charalambous and V. A. Kudryashov (1991). "The proximity effect in electron beam nanolithography." Microelectronic Engineering 13(1–4): 221-224.
Mark A. McCord and Michael J. Rooks. Electron beam lithography. In P. Rai Choudhury, editor, Handbook of Microlithography, Micromachining, and Microfabrica-tion, volume 1, chapter 2. SPIE Optical Engineering Press, London, 1997.

## Slide 12
Thank you