## Slide 1: Contrast Properties of Electron Beam Resist
Ahmed Al Balushi

## Slide 2: Overview
Resist materials
  Sensitivity
  Contrast
Development curves
Resist contrast
Conclusion
Q&A

## Slide 3: Resist Materials
Important properties of resist are:
  Sensitivity
  Contrast
    Linked to resolution capability of resist

## Slide 4
Sensitivity and contrast are derived from a resist development curves
Resist A has higher sensitivity
Resist A has higher contrast

## Slide 5: Development Curves
development curves, also called contrast curves, are obtained by exposure and development of a series of large square patterns with different exposure doses
The remaining resist thickness is measured against the exposure dose, which generates the development curves

## Slide 6: Resist Contrast
Resist contrast is defined by the slope of a development curve and expressed as:
where
  D1 is the exposure dose at which the resist is fully exposed
  D0 is the exposure dose at which the resist starts to be exposed
The steeper the slope, the higher the resist contrast

## Slide 7: Resist Contrast
The steeper the slope is, the higher the resist contrast.
Resist contrast is an inherent property of a resist material. However, development conditions can have some influence on it.

## Slide 8
Development curves of HSQ negative-tone resist exposed at different e-beam energies
Contrast curve of SU-8 resist

## Slide 9: Resist contrast
By the appearance of contrast curves of these two resists, one can immediately tell that the HSQ resist has higher contrast.
The contrast of negative-tone resist HSQ is 2.8
Another negative-tone resist, SU-8, has a contrast of only 0.92, as measured from contrast curve shown in the figure

## Slide 10: Resist Contrast
Apart from measuring the slope of resist contrast curves, another direct way of judging the resist contrast is to observe the resist profile after development.
High contrast resist

## Slide 11: Resist contrast
High contrast is always desirable because:
It enables resist profiles after development to have vertical sidewalls and high aspect ratios
  Facilitate pattern transfer
  Enable lithography of high density patterns

## Slide 12: Thank You Q&A