## Slide 1: Factors affecting the Depth of Field for SEM
Camtec workshop 2014
Aiko Kurimoto

## Slide 2: Definition of Depth of Field
Depth of Field (DOF)
  Distance between the nearest and farthest objects in a scene that appear acceptably sharp in an image.
Shallow DOF
Deep DOF

## Slide 3: DOF for SEM
Usually great DOF
This makes it possible to examine much rougher, and much higher magnifications, than is possible with optical microscopes.
Shallow DOF
Deep DOF

## Slide 4: Practical expression of DOF
α = the beam divergence
M = Magnification
Since
W = working distance between the lens and the specimen in mm.
A = the aperture diameter.

## Slide 5: Determination of DOF
W = working distance between the lens and the specimen in mm.
A = the aperture diameter.
M = Magnification
In order to increase DOF,
Increase the distance W
Decrease the size of A
Decrease the magnification M

## Slide 6: DECREASE APPERTURE SIZE
An increase DOF
A decrease the probe current and a concomitant decrease in S/N
Possible improvement in the probe size and resolution
Change in astigmatism (needs to be corrected again)

## Slide 7: INCREASE WORKING DISTANCE
  An increase DOF
  Lower attainable limits for low magnification work
  An increase probe size and thus less sharp but smoother image in appearance
  A possible decrease of signal strength (depending on stage tilt and detector position)
  Astigmatism will worsen at long W

## Slide 8: CONCLUSION
In order to increase DOF,
Increase the distance W
Decrease the size of A
Decrease the magnification M
However, an increase DOF involves some trade-offs. In order to obtain the best DOF, it is necessary to determine best combinations of the working distance, the aperture size and the magnification.