## Slide 1: Effect of Accelerating Voltage on Resolution
CAMTEC Nanofabrication Workshop
Mohammadreza Sanadgol Nezami
sanadgol@uvic.ca

## Slide 2: The instrument in brief
http://www.uio.no/studier/emner/matnat/fys/MENA3100/v09/lecture_notes/24february09.ppt

## Slide 3: How do we get an image?
In brief: we shoot high-energy electrons and analyze the outcoming electrons/x-rays
Electrons in
Electrons out
or: x-rays out
http://www.uio.no/studier/emner/matnat/fys/MENA3100/v09/lecture_notes/24february09.ppt

## Slide 4: How do we get an image?
156 electrons!
Image
Detector
Electron gun
288 electrons!
http://www.uio.no/studier/emner/matnat/fys/MENA3100/v09/lecture_notes/24february09.ppt

## Slide 5: Signals from the sample
Incoming electrons
Secondary electrons
Backscattered
electrons
Auger electrons
X-rays
Cathodo-
luminescence (light)
Sample
http://www.uio.no/studier/emner/matnat/fys/MENA3100/v09/lecture_notes/24february09.ppt

## Slide 6
Electron gun
Electron emitter

## Slide 7
Effects of increasing voltage in electron gun:
Resolution increased ( decreased)
Penetration increases
Specimen charging increases (insulators)
Specimen damage increases
Image contrast decreases
 = h/(2melectronqVo + q2Vo2/c2))

## Slide 8: Interaction Volume
The image details and resolution in the SEM are determined not by the size of the electron probe by itself but rather by the size and characteristics of the interaction volume.
The resulting region over which the incident electrons interact with the sample is known as interaction volume.
The energy deposition rate varies rapidly throughout the interaction volume, being greatest near the beam impact point.
The interaction volume has a distinct shape
For low-atomic-number target it has distinct pear shape.
For intermediate and high-atomic number materials the shape is in the form of hemi-sphere.
The interaction volume increases with increasing incident beam energy and
decreases with increasing average atomic number of the specimen.
For secondary electrons the sampling depth is from 10 to 100 nm and diameter equals the diameter of the area emitting backscattered electrons.
BSE are emitted from much larger depths compared to SE.
Ultimately the resolution in the SEM is controlled by the size of the interaction volume.

## Slide 9
http://www.medicine.mcgill.ca/femr/SEM%20Sample%20Prep%20JEOL.pdf

## Slide 10
http://www.polymer.hacettepe.edu.tr/webim/msen/undergraduate/NNT602/SEM_TEM.ppt

## Slide 11
Image: Department of Geology and Geophysics, Louisiana State University
Where does the signals come from?
Diameter of the interaction volume is larger than the electron spot
 resolution is poorer than the size of the electron spot
http://www.uio.no/studier/emner/matnat/fys/MENA3100/v09/lecture_notes/24february09.ppt0

## Slide 12: Electron beam-sample interactions
The incident electron beam is scattered in the sample, both elastically and inelastically
This gives rise to various signals that we can detect (more on that on next slide)
Interaction volume increases with increasing acceleration voltage and decreases with increasing atomic number
Images: Smith College Northampton, Massachusetts
http://www.uio.no/studier/emner/matnat/fys/MENA3100/v09/lecture_notes/24february09.ppt0

## Slide 13: Effects of accelerating voltage

## Slide 14
 = h / (2melectronqVo + q2Vo2/c2)1/2
 = 1.22639 / (Vo + 0.97845 · 10-6Vo2)1/2
(nm) & Vo(volts)
10 kV ——> 0.12 Å
100 kV ——> 0.037 Å

## Slide 15
http://www.medicine.mcgill.ca/femr/SEM%20Sample%20Prep%20JEOL.pdf

## Slide 17
Thank you!